Briefed explanation of the document:

The standards institution of Israel

Israeli standard   I.S №.3   August 1988

Mineral aggregates from natural sources

Foreign document:

ASTM C 40     Standard test method for organic impurities in fine aggregates for concrete

Definition:

Natural fine aggregate for concrete (natural sand 06/015)

The Classification by sieve size

(Sieve size means the nominal eye diameter):

Table № 3

90% - 100% pass trough sieve size 0.6   mm

40% - 80% pass through sieve size 0.3   mm

0%   - 10% pass through sieve size 0.15 mm

Table № 4

Maximum dust content:  1% by weight.

Maximum Clay content 0.5% by weight.

Organic impurity content: Will not change color through  ASTM C 40 -1992 test.

Maximum absorbency: 1%  by weight