## Uranium (U ) by %

Uranium (U) Element Properties Atomic Mass 238.0289 Atomic Number 92 Name Origins Named after the planet Uranus. Year Discovered 1789 Discovery Credits Discovered by M. H. Klaproth at Berlin, German; isolated in 1841 by E. M. Pleigot at Paris, France Remarks Radioactive silvery metal. malleable, ductile, and tarnishes in air. Attacked by steam and acids but not by alkalis. Used as nuclear fuel and in nuclear weapons. Diagnostic tests: Uranium is usually detected by radioactivity (due, in part, to the daughter elements such as radium). Thorium is also naturally radioactive; however, many uranium minerals are generally yellow or green and fluorescent. With a borax bead test in the oxidizing flame, the bead is yellow to brownish red color while hot and is colorless to yellow when cold. This test is very similar to iron. The Na2(NH4)(PO4) bead test for uranium is a much better test, under oxidizing conditions the bead is clear yellow (hot) yielding slightly greenish yellow on cooling. In the reducing flame, it becomes a fine green color when hot or cold. References Emsley, J., 1991; THE ELEMENTS : Sec. Ed., Clarendon Press, Oxford, 251 p. See Also WebElements, ChemiCool Naturally Occurring Isotopes Symbol Isotope Mass Isotope Nuclide Number Isotope Number Natural Abundance Half-life Half-life Units Decay Mode Decay Mode MeV Decay Mode % U 234.040946 234 92 0.0050% 245,000 Years alpha 4.856 100.00% U 235.043924 235 92 0.7200% 7x108 Years alpha 4.6793 100.00% U 236.045562 236 92 0.0000% 2x107 Years alpha 4.569 100.00% U 238.050784 238 92 99.2750% 4x109 Years alpha 4.039 100.00% Mineral Species sorted by the element U (Uranium ) Click Here for Mineral Species Sorted By Mineral Name %U Mineral Name Chemical Formula MW 88.15%U Uraninite UO2 270.03 78.29%U IMA2008-022 UO2(OH)2 304.04 78.29%U Ianthinite (UO2)•5(UO3)•10(H2O) 304.04 76.04%U Metaschoepite UO3•n(H2O)(n<2) 313.05 73.91%U Paraschoepite UO3•2(H2O)(?) 322.06 72.89%U Schoepite (UO2)8O2(OH)12•12(H2O) 2,612.49 72.63%U Coffinite U(SiO4)1-x(OH)4x 327.71 72.48%U Becquerelite Ca(UO2)6O4(OH)6•8(H2O) 1,970.41 72.26%U Metauranopilite (UO2)6(SO4)(OH)10•5(H2O) 1,976.38 72.12%U Rutherfordine UO2(CO3) 330.04 71.48%U Agrinierite (K2,Ca,Sr)U3O10•4(H2O) 998.94 71.25%U Soddyite (UO2)2SiO4•2(H2O) 668.17 71.11%U Compreignacite K2(UO2)6O4(OH)6•8(H2O) 2,008.53 70.41%U Metastudtite UO4•2(H2O) 338.06 70.40%U Rameauite K2CaU++++++6O20•9(H2O) 2,028.57 69.79%U Jachymovite ! (UO2)8(SO4)(OH)14•13(H2O) 2,728.59 69.58%U Metacalciouranoite (Ca,Na,Ba)U2O7•2(H2O) 718.40 69.27%U Metavandendriesscheite PbU7O22•n(H2O)(n<12) 2,405.54 69.19%U Metavanmeersscheite U++++++(UO2)3(PO4)2(OH)6•2(H2O) 1,376.13 69.07%U Billietite Ba(UO2)6O4(OH)6•8(H2O) 2,067.66 68.80%U Nielsbohrite ! K(UO2)3(AsO4)(OH)4•H2O 1,093.26 68.39%U Blatonite ! UO2CO3•(H2O) 348.05 68.38%U Natroboltwoodite (H3O)(Na,K)(UO2)SiO4•(H2O) 696.19 67.93%U Uranopilite [(UO2)6(SO4)O2(OH)6(H2O)6]•8(H2O) 2,102.49 67.77%U Wyartite Ca3U++++(UO2)6(CO3)2(OH)18•3-5(H2O) 2,458.63 67.76%U Vandendriesscheite Pb(UO2)10O6(OH)11•11(H2O) 3,513.04 67.42%U Vanmeersscheite U++++++(UO2)3(PO4)2(OH)6•4(H2O) 1,412.16 67.42%U Oswaldpeetersite ! (UO2)2CO3(OH)2•4(H2O) 706.14 67.40%U Coutinhoite ! ThxBa1-2x(H2O)y(UO2)2Si5O13•H2O 2,118.94 67.21%U Clarkeite (Na,Ca,Pb)(UO2)O(OH)•0-1(H2O) 318.75 66.97%U Urancalcarite Ca(UO2)3(CO3)(OH)6•3(H2O) 1,066.26 66.85%U Sharpite Ca(UO2)6(CO3)5(OH)4•6(H2O) 2,136.41 66.15%U Richetite PbU++++++4O13•4(H2O) 1,439.37 65.91%U Protasite Ba(UO2)3O3(OH)2•3(H2O) 1,083.47 65.02%U Joliotite (UO2)(CO3)•n(H2O),(n=2?) 366.07 64.68%U Lermontovite U++++(PO4)(OH)•(H2O)(?) 368.02 64.53%U Fourmarierite Pb(UO2)4O3(OH)4•4(H2O) 1,475.40 64.32%U Fontanite Ca[(UO2)3(CO3)2O2]•6(H2O) 1,110.27 63.99%U Lepersonnite-(Gd) CaGd2(UO3)24(CO3)8(SiO4)4O4•60(H2O) 8,909.01 63.90%U Yingjiangite (K2,Ca)(UO2)7(PO4)4(OH)6•6(H2O) 2,607.53 63.79%U Holfertite ! U++++++1.75TiCa0.25O7.5(H2O)3 649.27 63.73%U Phosphuranylite KCa(H3O)3(UO2)7(PO4)4O4•8(H2O) 2,614.45 63.63%U Studtite [(UO2)O2(H2O)2](H2O)2 374.09 63.47%U Arsenovanmeersscheite U(OH)4[(UO2)3(AsO4)2(OH)2]•4H2O 1,500.06 63.34%U Curite Pb3+x(H2O)2[(UO2)4+x(OH)3-x]2,x~0.5 3,006.49 63.01%U Magnesiozippeite Mg(H2O)3.5(UO2)2(SO4)O2 755.48 62.74%U Tengchongite CaU++++++6Mo++++++2O25•12(H2O) 2,276.30 62.54%U Rabejacite Ca(UO2)4(SO4)2(OH)6•6(H2O) 1,522.45 61.91%U Masuyite Pb[(UO2)3O3(OH)2]•3(H2O) 1,153.34 61.91%U Zippeite K4(UO2)6(SO4)3(OH)10•4(H2O) 2,306.88 61.26%U Francoisite-(Nd) (Nd,Y,Sm,Ce)(UO2)3(PO4)2O(OH)•6(H2O) 1,243.40 61.13%U Mundite Al(UO2)3(PO4)2(OH)3•5(H2O) 1,168.11 60.70%U Uranophane-beta Ca[(UO2)SiO3(OH)]2•(H2O) 784.33 60.58%U Calciouranoite (Ca,Ba,Pb)U2O7•5(H2O) 667.92 60.52%U Sayrite Pb2(UO2)5O6(OH)2•4(H2O) 1,966.61 60.48%U Arsenuranylite Ca(UO2)4(AsO4)2(OH)4•6(H2O) 1,574.15 60.42%U Chadwickite ! (UO2)H(AsO3) 393.96 60.25%U Vyacheslavite U++++(PO4)(OH)•2.5(H2O) 395.05 60.20%U Upalite Al(UO2)3(PO4)2O(OH)•7(H2O) 1,186.12 60.10%U Haynesite (UO2)3(SeO3)2(OH)2•5(H2O) 1,188.09 59.99%U Wolsendorfite (Pb,Ba,Ca)U2O7•2(H2O) 793.61 59.74%U Roubaultite Cu2(UO2)3(CO3)2O2(OH)2•4(H2O) 1,195.27 59.52%U Larisaite ! Na(H3O)(UO2)3(SeO3)2O2•4(H2O) 1,235.71 59.27%U Vandenbrandeite Cu(UO2)(OH)4 401.60 59.24%U Marecottite ! Mg3(H2O)18[(UO2)4O3(SO4)2]2•10(H2O) 3,310.81 59.10%U Spriggite ! Pb3[(UO2)6O8(OH)2](H2O)x;x~3 2,424.63 59.03%U Bauranoite BaU2O7•4-5(H2O) 806.45 58.09%U Natrozippeite Na4(UO2)6(SO4)3(OH)10•4(H2O) 2,458.63 57.77%U Althupite ThAl(UO2)7(PO4)4(OH)5•15(H2O) 2,884.36 57.67%U Phurcalite Ca2(UO2)3O2(PO4)2•7(H2O) 1,238.29 57.49%U Nickelzippeite Ni++2(UO2)6(SO4)3(OH)10•16(H2O) 2,484.05 57.48%U Cobaltzippeite Co++2(UO2)6(SO4)3(OH)10•16(H2O) 2,484.54 57.39%U Piretite ! Ca(UO2)3(SeO3)2(OH)4-4(H2O) 1,244.17 57.34%U IMA2009-008 Y2[(UO2)8O6(SO4)4(OH)2]•26H2O 3,320.70 57.19%U Zinc-zippeite Zn++2(UO2)6(SO4)3(OH)10•16(H2O) 2,497.45 56.97%U Renardite Pb(UO2)4(PO4)2(OH)4•7(H2O) 1,671.39 56.71%U Kamitugaite PbAl(UO2)5(PO4)2(OH)9•9.5(H2O) 2,098.47 56.53%U Meta-autunite Ca(UO2)2(PO4)2•2-6(H2O) 842.14 56.34%U Swamboite U++++++H6(UO2)6(SiO4)6•30(H2O) 2,957.20 56.12%U Francoisite-(Ce) ! (Ce,Nd,Ca)[(UO2)3O(OH)(PO4)2]•6(H2O) 1,272.47 55.80%U Kivuite ? (Th,Ca,Pb)H2(UO2)4(PO4)2(OH)8•7(H2O) 1,706.20 55.48%U Triangulite Al3(UO2)4(PO4)4(OH)5•5(H2O) 1,716.05 55.47%U Guilleminite Ba(UO2)3(SeO3)2O2•3(H2O) 1,287.37 55.45%U Boltwoodite HK(UO2)(SiO4)•1.5(H2O) 429.24 55.44%U Sklodowskite (H3O)2Mg(UO2)2(SiO4)2•4(H2O) 858.63 55.24%U Cuprosklodowskite Cu[(UO2)(SiO2OH)]2•6(H2O) 861.84 55.10%U Metatyuyamunite Ca(UO2)2V2O8•3(H2O) 864.06 54.78%U Marthozite Cu[(UO2)3(SeO3)2O2]•8(H2O) 1,303.67 54.61%U Oursinite (Co,Mg)(H3O)2[(UO2)SiO4]2•3(H2O) 871.78 54.46%U Uramphite (NH4)(UO2)(PO4)•3(H2O) 437.08 54.34%U Deliensite ! Fe++(UO2)2(SO4)2(OH)2•3(H2O) 876.09 54.34%U Chernikovite (H3O)2(UO2)2(PO4)2•6(H2O) 876.14 53.88%U Bijvoetite-(Y) (Y,REE)8(H2O)25(UO2)16O8(OH)8(CO3)16•14(H2O) 7,068.68 53.60%U Sabugalite HAl(UO2)4(PO4)4•16(H2O) 1,776.23 53.44%U Phuralumite Al2(UO2)3(PO4)2(OH)6•10(H2O) 1,336.19 53.41%U Schmitterite (UO2)TeO3 445.63 53.28%U Orthobrannerite U++++U++++++Ti4O12(OH)2 893.59 53.20%U Vanuranylite ? (H3O,Ba,Ca,K)1.6(UO2)2V2O8•4(H2O)(?) 894.90 53.19%U Kamotoite-(Y) (Y,Nd,Gd)2U++++++4(CO3)3O12•14.5(H2O) 1,790.08 53.13%U Umohoite [(UO2)MoO4]•H2O 447.98 52.77%U Sodium meta-autunite ! Na2(UO2)2(PO4)2•6-8(H2O) 902.08 52.77%U Carnotite K2(UO2)2V2O8•3(H2O) 902.18 52.72%U Vochtenite (Fe++,Mg)Fe+++[(UO2)(PO4)]4(OH)•12-13(H2O) 1,806.00 52.08%U Pseudojohannite ! Cu6.5[(UO2)4O4(SO4)2]2(OH)5•25H2O 3,587.89 51.96%U Meta-ankoleite K2(UO2)2(PO4)2•6(H2O) 916.29 51.85%U Tyuyamunite Ca(UO2)2V2O8•5-8(H2O) 918.10 51.85%U Threadgoldite Al(UO2)2(PO4)2(OH)•8(H2O) 918.11 51.74%U Sodium-autunite Na2(UO2)2(PO4)2•8(H2O) 920.10 51.52%U Strelkinite Na2(UO2)2V2O8•6(H2O) 924.00 51.50%U Ningyoite (U,Ca,Ce)2(PO4)2•1-2(H2O) 554.67 51.40%U Uramarsite ! (NH4,H3O)2(UO2)2(AsO4,PO4)2•6H2O 935.42 51.24%U Lehnerite Mn[UO2/PO4]2•8(H2O) 929.06 51.19%U Bassetite Fe++(UO2)2(PO4)2•8(H2O) 929.97 50.94%U Saleeite Mg(UO2)2(PO4)2•10(H2O) 934.46 50.77%U Metatorbernite Cu(UO2)2(PO4)2•8(H2O) 937.67 50.10%U Metanovacekite Mg(UO2)2(AsO4)2•4-8(H2O) 950.29 49.98%U Natrouranospinite (Na2,Ca)(UO2)2(AsO4)2•5(H2O) 952.47 49.69%U Metavanuralite Al(UO2)2(VO4)2(OH)•8(H2O) 958.04 49.67%U Xiangjiangite (Fe+++,Al)(UO2)4(PO4)2(SO4)2(OH)•22(H2O) 1,916.94 49.38%U Trogerite H2(UO2)2(AsO4)2•8(H2O) 964.03 49.18%U Dewindtite Pb3[H(UO2)3O2(PO4)2]2•12(H2O) 2,903.85 49.16%U Metazellerite Ca(UO2)(CO3)2•3(H2O) 484.17 49.10%U Chistyakovaite-(Y) ! Al(UO2)2(AsO4)2(F,OH)•6.5H2O 969.53 48.88%U Johannite Cu(UO2)2(SO4)2(OH)2•8(H2O) 973.87 48.84%U Margaritasite (Cs,K,H3O)2(UO2)2V2O8•(H2O) 974.70 48.64%U Francevillite (Ba,Pb)(UO2)2V2O8•5(H2O) 978.77 48.58%U Weeksite K2(UO2)2Si6O15•4(H2O) 1,028.91 48.27%U Autunite Ca(UO2)2(PO4)2•10-12(H2O) 986.26 48.00%U Torbernite Cu(UO2)2(PO4)2•8-12(H2O) 991.71 47.92%U Metauranocircite Ba(UO2)2(PO4)2•6-8(H2O) 993.43 47.65%U Fritzscheite Mn(UO2)2[(V,P)O4]2•4(H2O) 999.03 47.58%U Haiweeite Ca[(UO2)2Si5O12(OH)2]•3(H2O) 1,000.61 47.51%U Metauranospinite Ca(UO2)2(AsO4)2•8(H2O) 1,002.09 47.36%U Sengierite Cu2(UO2)2V2O8•6(H2O) 1,005.12 47.21%U Cousinite MgU2Mo2O13•6(H2O)(?) 1,008.33 47.17%U Przhevalskite Pb(UO2)2(PO4)2•4(H2O) 1,009.26 47.04%U Vanuralite Al(UO2)2(VO4)2(OH)•11(H2O) 1,012.09 46.77%U Metakahlerite Fe++(UO2)2(AsO4)2•8(H2O) 1,017.86 46.64%U Metarauchite ! Ni(UO2)2(AsO4)2•8H2O 1,020.71 46.63%U Metakirchheimerite Co(UO2)2(AsO4)2•8(H2O) 1,020.95 46.47%U Dumontite Pb2(UO2)3O2(PO4)2•5(H2O) 1,536.50 46.42%U Metazeunerite Cu(UO2)2(AsO4)2•8(H2O) 1,025.56 46.12%U Ranunculite HAl(UO2)(PO4)(OH)3•4(H2O) 516.07 46.05%U Metahaiweeite Ca(UO2)2Si6O15•n(H2O),n<5 1,033.68 45.86%U Uranospinite Ca(UO2)2(AsO4)2•10(H2O) 1,038.12 45.77%U Abernathyite K(UO2)(AsO4)•4(H2O) 520.11 45.76%U Zellerite Ca(UO2)(CO3)2•5(H2O) 520.20 45.71%U Calcurmolite Ca(UO2)3(MoO4)3(OH)2•11(H2O) 1,562.16 45.08%U Uranosphaerite Bi(UO2)O2(OH) 528.01 44.98%U Novacekite Mg(UO2)2(AsO4)2•12(H2O) 1,058.38 44.87%U Cejkaite ! Na4(UO2)(CO3)3 546.35 44.84%U Zeunerite Cu(UO2)2(AsO4)2•10-16(H2O) 1,061.59 44.77%U Metalodevite Zn(UO2)2(AsO4)2•10(H2O) 1,063.44 44.61%U Curienite Pb(UO2)2V2O8•5(H2O) 1,067.21 44.41%U Kahlerite Fe++(UO2)2(AsO4)2•10-12(H2O) 1,071.91 43.96%U Hugelite Pb2(UO2)3(AsO4)2(OH)4•3(H2O) 1,624.40 43.94%U Uranocircite Ba(UO2)2(PO4)2•12(H2O) 1,083.51 43.42%U Seelite-2 Mg(UO2)(AsO3)x(AsO4)1-x•7(H2O)(x=0.7) 548.16 43.30%U Metaheinrichite Ba(UO2)2(AsO4)2•8(H2O) 1,099.34 43.28%U Bergenite Ca2Ba4[(UO3)2O2(PO4)2]3(H2O)16 3,299.70 42.99%U Sreinite ! Pb2(UO2)11(BiO)8(PO4)5(OH)19•6(H2O) 6,090.63 42.66%U Sedovite U(MoO4)2 557.90 42.50%U Asselbornite (Pb,Ba)(UO2)6(BiO)4(AsO4)2(OH)12•3(H2O) 3,237.04 42.12%U Uranospathite Al1-x[]x[(UO2)(PO4)]2(H2O)20+3xF1-3x 1,130.30 42.11%U Ursilite * (Mg,Ca)4[(UO2)4(OH)5/(Si2O5)5.5]•13(H2O) 2,261.26 41.27%U Heinrichite Ba(UO2)2(AsO4)2•10-12(H2O) 1,153.39 41.16%U Liandratite U++++++(Nb,Ta)2O8 578.25 40.82%U Pseudo-autunite * (H3O)4Ca2(UO2)2(PO4)4•5(H2O)(?) 1,166.27 40.77%U Uranotungstite (Fe++,Ba,Pb)(UO2)2WO4(OH)4•12(H2O) 1,167.54 40.59%U Uranophane Ca(UO2)2SiO3(OH)2•5(H2O) 586.36 40.53%U Kasolite Pb(UO2)SiO4•(H2O) 587.33 39.93%U Arsenuranospathite HAl(UO2)4(AsO4)4•40(H2O) 2,384.39 39.13%U Grimselite K3Na(UO2)(CO3)3•(H2O) 608.36 39.11%U Romanite * (Fe++,U,Pb)2(Ti,Fe+++)O4 365.14 38.34%U Seelite-1 Mg[(UO2)(AsO3)x(AsO4)1-x]2•7(H2O) 620.82 38.15%U Moluranite H4U++++(UO2)3(MoO4)7•18(H2O) 2,495.98 37.91%U Iriginite (UO2)(Mo++++++2O7)•3(H2O) 627.95 37.45%U Ulrichite CaCu(UO2)(PO4)2•4(H2O) 635.66 36.95%U Andersonite Na2Ca(UO2)(CO3)3•6(H2O) 644.20 36.52%U Petscheckite U++++Fe++(Nb,Ta)2O8 651.70 34.79%U Lakebogaite ! CaNaFe+++2H(UO2)2(PO4)4(OH)2(H2O)8 1,231.53 34.35%U Uranopolycrase (U,Y)(Ti,Nb,Ta)2O6 415.77 34.30%U Uvanite U++++++2V+++++6O21•15(H2O) 1,387.92 33.69%U Uranosilite (U++++++O2)Si7O15 706.62 33.54%U Brannerite (U,Ca,Ce)(Ti,Fe)2O6 354.80 33.31%U Albrechtschraufite Ca4Mg(UO2)2(CO3)6F2•17(H2O) 1,428.98 32.68%U Liebigite Ca2(UO2)(CO3)3•11(H2O) 728.38 32.58%U Swartzite CaMg(UO2)(CO3)3•12(H2O) 730.62 32.05%U Rabbittite Ca3Mg3(UO2)2(CO3)6(OH)4•18(H2O) 1,485.56 31.24%U Voglite Ca2Cu(UO2)(CO3)4•6(H2O) 761.86 31.12%U Cliffordite UTe3O9 764.82 30.91%U Coconinoite Fe+++2Al2(UO2)2(PO4)4(SO4)(OH)2•18(H2O) 1,539.95 30.74%U Tristramite (Ca,U++++,Fe+++)(PO4,SO4)•2(H2O) 232.32 30.24%U Furongite Al2(UO2)(PO4)3(OH)2•8(H2O) 787.04 28.92%U Bayleyite Mg2(UO2)(CO3)3•18(H2O) 822.94 28.73%U Moctezumite Pb(UO2)(TeO3)2 828.42 27.54%U Widenmannite Pb2(UO2)(CO3)3 864.46 27.37%U Uranmicrolite (U,Ca)2(Ta,Nb)2O6(OH) 695.81 27.04%U Derriksite Cu4(UO2)(SeO3)2(OH)6 880.17 26.79%U Schrockingerite NaCa3(UO2)(CO3)3(SO4)F•10(H2O) 888.49 26.33%U Moreauite Al3(UO2)(PO4)3(OH)2•13(H2O) 904.10 26.15%U Parsonsite Pb2(UO2)(PO4)2•2(H2O) 910.40 26.07%U Rauvite Ca(UO2)2V+++++10O28•16(H2O) 1,825.78 25.16%U Deloryite Cu++4(UO2)(MoO4)2(OH)6 946.13 25.02%U Astrocyanite-(Ce) Cu2(Ce,Nd,La)2(UO2)(CO3)5(OH)2•1.5(H2O) 951.38 24.74%U Hallimondite Pb2(UO2)(AsO4)2 962.27 24.54%U Shabaite-(Nd) Ca(Nd,Sm,Y)2(UO2)(CO3)4(OH)2•6(H2O) 969.96 24.36%U Thorutite (Th,U,Ca)Ti2(O,OH)6 390.82 24.25%U Ishikawaite (U,Fe,Y,Ca)(Nb,Ta)O4(?) 294.45 22.04%U Mourite U++++Mo++++++5O12(OH)10 1,079.80 21.92%U Demesmaekerite Pb2Cu5(UO2)2(SeO3)6(OH)6•2(H2O) 2,172.01 20.73%U Ashanite ? (Nb,Ta,U,Fe,Mn)4O8 574.20 17.59%U Uranpyrochlore (U,Ca,Ce)2(Nb,Ta)2O6(OH,F) 541.23 17.20%U Betafite (Ca,U)2(Ti,Nb,Ta)2O6(OH) 415.12 16.05%U Yttrocolumbite-(Y) (Y,U,Fe++)(Nb,Ta)O4 296.62 16.04%U Orthowalpurgite (UO2)Bi4O4(AsO4)2•2(H2O) 1,483.82 16.04%U Walpurgite Bi4(UO2)(AsO4)2O4•2(H2O) 1,483.82 15.88%U Samarskite-(Y) (Y,Fe+++,U)(Nb,Ta)5O4 299.85 15.56%U Phosphowalpurgite ! (UO2)Bi4(PO4)O4•2(H2O) 1,391.69 14.68%U Znucalite CaZn11(UO2)(CO3)3(OH)20•4(H2O) 1,621.63 14.58%U Arapovite ! (U,Th)(Ca,Na)2(K1-x[]x)Si8O20•H2O,x=0.5 897.66 12.69%U Bismutopyrochlore ! (Bi,U,Ca,Pb)1+x(Nb,Ta)2O6(OH)•n(H2O) 562.81 12.47%U Cleusonite ! Pb(U++++,U++++++)(Ti,Fe++,Fe+++)20(O,OH)38 2,080.74 11.18%U Plumbobetafite (Pb,U,Ca)(Ti,Nb)2O6(OH,F) 425.90 10.44%U Yttropyrochlore-(Y) (Y,Na,Ca,U)1-2(Nb,Ta,Ti)2(O,OH)7 455.99 9.60%U Samarskite-(Yb) ! (Yb,Y,REE,U,Th,Ca,Fe++)(Nb,Ta,Ti)O4 312.29 7.99%U Yttrocrasite-(Y) (Y,Th,Ca,U)(Ti,Fe+++)2(O,OH)6 298.05 7.54%U Yttrotantalite-(Y) (Y,U,Fe++)(Ta,Nb)O4 315.74 7.46%U Kobeite-(Y) (Y,U)(Ti,Nb)2(O,OH)6(?) 319.10 6.38%U Polycrase-(Y) (Y,Ca,Ce,U,Th)(Ti,Nb,Ta)2O6 372.96 6.04%U Calciobetafite Ca2(Ti,Nb)2(O,OH)7 394.30 5.99%U Plumbomicrolite (Pb,Ca,U)2Ta2O6(OH) 795.19 5.45%U Yttrobetafite-(Y) (Y,U,Ce)2(Ti,Nb,Ta)2O6(OH) 437.15 4.92%U Plumbopyrochlore (Pb,Y,U,Ca)2-xNb2O6(OH) 484.00 3.85%U Dessauite ! (Sr,Pb)(Y,U)(Ti,Fe+++)20O38 1,856.57 3.20%U Davidite-(La) (La,Ce,Ca)(Y,U)(Ti,Fe+++)20O38 1,860.86 3.18%U Davidite-(Ce) (Ce,La)(Y,U)(Ti,Fe+++)20O38 1,871.41 1.87%U Lakargiite ! CaZrO3 177.87 0.76%U Iwashiroite-(Y) ! YTaO4 313.16 0.69%U Ciprianiite ! Ca4[(Th,U)(REE)]2(Al,[])2[Si4B4O22](OH,F)2 1,032.51 0.64%U Piergorite-(Ce) ! Ca8Ce2(Al0.5 Fe+++0.5)([ ],Li,Be)2Si6B8O36(OH,F)2 1,498.89 0.58%U Nioboaeschynite-(Y) ! [(Y,REE),Ca,Th,Fe](Nb,Ti,Ta)2(O,OH)6 368.70 0.36%U Sazhinite-(La) ! Na3La[Si6O15]•2(H2O) 652.93 0.35%U Kapustinite ! Na5.5Mn0.25ZrSi6O16(OH)2 689.44 0.26%U Gramaccioliite-(Y) ! (Pb,Sr)(Y,Mn)Fe2(Ti,Fe)18O38 1,822.46 0.17%U Menezesite ! Ba2MgZr4(BaNb12O42)•12H2O 2,778.48 0.13%U Dissakisite-(La) ! (Ca,Fe++,Th, La)(La,REE,Ca)(Al,Cr,Ti)2(Mg,Fe,Al)Si3O12(OH,F) with La > Ce 551.33 0.09%U Okanoganite-(Y) (Na,Ca)3(Y,Ce)12Si6B2O27F14 2,660.88 0.01%U Stornesite-(Y) ! (Y, Ca)[ ]2Na6(Ca,Na)8(Mg,Fe)43(PO4)36 5,318.15 (* - Mineral Name Is Not IMA Approved) (! - New Dana classification added or changed from Danas New Mineralogy) (? - IMA Discredited Mineral Species Name) There are 249 minerals with U in the Mineralogy Database.